Control Number:     A070006

Category:      Asbestos

EPA Office:    CAMPD

Date:          01/31/2007

Title:         Rounding Reported Values

Recipient:     Zlatic, Michael

Author:        Alushin, Michael

Comments:

Subparts:      Part 61     M     Asbestos

References:    Part 763, Subpart E, Appendix E, Section 1

61.141

Abstract:

Q:  Could EPA clarify to the Saint Louis County Health Department in Missouri

how best to interpret the following phrase in 40 CFR part 63, subpart E: "the

value reported should be rounded to the nearest percent", in connection with

point counting results to determine the percentage of asbestos as between 1.0

percent and 1.5 percent and defining Category I and Category II nonfriable

asbestos-containing material (ACM)?

A:  EPA explains that when a bulk sample is analyzed using Polarized Light

Microscopy, and further quantified using the point counting method/formula in

40 CFR Part 763, Subpart E, Appendix E, Section 1.7.2.4, sample results are

allowed to be rounded to the nearest percent.  EPA interprets the rounding of

results using the formula in Section 1.7.2.4 as, if the sample result yields

a=4, Â?aÂ? being the number of asbestos counts, the result is 1 percent, which

does not meet the regulatory threshold of greater than 1 percent.  If the

sample result yields a=5, the result is 1.25 percent asbestos, which may be

rounded down to 1 percent, which is not greater than 1 percent and therefore

not regulated.  If the sample result yields a=6, the result is 1.5 percent

asbestos, which would be rounded to 2 percent and therefore regulated.

Letter:

January 31, 2007

Mr. Michael A. Zlatic, P.E.

Chief Environmental Engineer

Saint Louis County Health Department

Division of Environmental Protection

111 South Meramec Avenue

St. Louis, MO  63105

Dear Mr. Zlatic:

This responds to your letter of May 22, 2006 in which you request an EPA

determination that addresses how the following sentence found in 40 CFR Part

763, Subpart  E, Appendix E, section 1.7.2.4 should be implemented:  "The value

reported should be  rounded to the nearest percent."  You specifically ask how

this sentence should be  interpreted in connection with point counting results

placing the percentage of asbestos as  between 1.0% and 1.5% because the

asbestos NESHAP specifically defines Category I and  Category II nonfriable

asbestos-containing material (ACM), in relevant part, as "containing  more than

1 percent asbestos as determined using the methods specified in Appendix E,

Subpart E, 40 CFR Part 763, section 1, Polarized Light Microscopy,:

The sentence at issue first appeared in EPA's regulations in 1982.  On May 27th

of  that year, EPA promulgated a Final Rule entitled Friable

Asbestos-Containing Materials in  Schools; Proposed Identification and

Notification  (47 FR 23360).  In that final rule, EPA  took a document

originally entitled Interim Method for the Determination of Asbestiform

Minerals in Bulk Insulation Samples, which had been referenced in EPA's

proposed rule, and  made it an appendix (specifically, Appendix A - Interim

Method of the Determination of  Asbestos in Bulk Insulation Samples) to the

final regulatory text.  Subsequently, when  these regulations were amended in

1987, becoming EPA's current Asbestos-Containing  Materials in Schools

regulations (40 CFR Part 763, Subpart E), what was formerly Appendix A  became,

with some modification, Appendix E.  The sentence at issue previously was found

in  Appendix A and is included in the current Appendix E, Subpart E.

In responding to your inquiry, my staff researched previous Federal Register

Notices, Agency guidance documents, and files from Docket # OPTS 61004B;

TSH-FRL 2064-3  (the docket for the Agency's 1982 Final Rule promulgating the

Friable Asbestos-Containing  Materials in Schools regulations).  They did not

locate any specific reference in these  materials discussing the sentence in

Section 1.7.2.4.  However, there are discussions in  several documents in this

docket regarding the variability of sample results analyzed by different

laboratories.  Based on results of sampling analysis by commercial and

non-commercial  laboratories, the  Agency determined that the technical

capability of the microscopist was crucial for proper  sample analysis.  In

order to improve the sample analysis results by the microscopist, the  Agency

developed the previously mentioned document entitled Interim Method for the

Determination of Asbestiform Minerals in Bulk Insulation Samples.  In addition,

the Agency  worked with the Department of Commerce to develop a laboratory

accreditation program to  ensure accurate sample analysis.

Based on our research, it is EPA's position that when a bulk sample is analyzed

using Polarized Light Microscopy, and further quantified using the point

counting method,  40 CFR Part 763, Subpart E, Appendix E, section 1.7.2.4

(specifically, the sentence for  which you are seeking clarification) allows

for the rounding of such results to the nearest  percent.  For example, if the

percent asbestos is calculated for a sample using the formula  set forth in

Section 1.7.2.4 - i.e., % asbestos = (a/n) 100%, where a=number of asbestos

counts and n= number of nonempty points counted (400) -- and the sample result

yields a=4,  the result is 1% asbestos, which does not meet the greater than 1%

asbestos regulatory  threshold for ACM.  If a sample result yields a=5, the

result is 1.25% asbestos.  In this  case, section 1.7.2.4 of Appendix E allows

rounding of the result to 1%.  Accordingly, if  rounded, this result does not

meet the greater than 1% regulatory threshold for ACM.  If  the sample result

yields a=6, the result is 1.5% asbestos.  In rounding this sample result  to

the nearest percent, the result is 2% asbestos.  This sample result is greater

than 1%  and therefore the tested material qualifies as ACM.

The Office of Civil Enforcement, the Office of Air Quality Planning and

Standards,  the Office of Prevention, Pesticides and Toxic Substances and the

Office of General Counsel  have reviewed this determination.

Very truly yours,

Michael S. Alushin

Compliance Assessment and Media Programs Division

Office of Compliance

cc:  Tahani Rivers, OCE

Susan Fairchild, OAQPS

Chris Kaczmarek, OGC

Cindy Wheeler, OPPTS

Ellen Stough, OCEFT

Lynn Slugantz, Region 7